## Slide 1: Time dependent problems in superconductivity – some recent advances
Predrag Miranović
University of Montenegro

## Slide 2: Phenomenological approach – Time dependent Meissner effect
What will happen if applied magnetic field is time dependent:
Vladimir G. Kogan and Ruslan Prozorov, „Anisotropic time-dependent London approach: Application to the ac response in the Meissner state“, Phys. Rev. B 102, 184514 (2020)

## Slide 3: Electromagnetic wave scattering on superconducting sample –work in progress
Assumption: applied magnetic field ( wrong!)
Linearly polarized electromagnetic wave scattering on superconducting sphere (Mie scattering), exactly solvable.
Force acting on superconducting sphere by low frequency
EM field
EM field torque on superconducting sphere
Linearly polarized EM plane wave has no angular momentum, but
superconducting sphere is gaining momentum !?
What happens if circulary polarized electromagnetic wave fall on superconductor?

## Slide 4: Inverse Faraday effect
Faraday effect: EM wave polarization plane rotated by static magnetic field
Inverse Faraday effect: Static magnetization created by circulary polarized EM wave: (high frequency approximation)
Riccardo Hertel, Theory of the inverse Faraday effect in metals, Journal of Magnetism and Magnetic Materials 303 (2006) L1–L4

## Slide 5: Inverse Faraday effect in superconductors – phenomenological GL approach I
Time dependent Ginzburg-Landau equations
S. V. Mironov, A. S. Mel’nikov, I. D. Tokman, V. Vadimov, B. Lounis, and A. I. Buzdin, „Inverse Faraday Effect for Superconducting Condensates “, Phys. Rev. Lett. 126, 137002 (2021)
Linear in field correction that originates from the nonlinear EM field correction of order parameter

## Slide 6: Inverse Faraday effect in superconductors – phenomenological GL approach II
Disc volume V, radius R, thickness L. EM wave intensity I.
High frequency approximation
S. V. Mironov, A. S. Mel’nikov, I. D. Tokman, V. Vadimov, B. Lounis, and A. I. Buzdin, „Inverse Faraday Effect for Superconducting Condensates “, Phys. Rev. Lett. 126, 137002 (2021)
Low frequency approximation

## Slide 7: Microscopic approach to time dependent phenomena in superconductors
Main task is to find kernel beyond the linear response theory
Keldysh Green’s function technique for nonequilibrium superconductivity
Retarded , Advanced , and Keldysh Green functions, elements of Nambu-Keldysh 8x8 propagator
D. Rainer and J. A. Sauls, Strong-Coupling Theory of Superconductivity, Superconductivity: From Basic Physics to New Developments, arXiv: 1809.05264.

## Slide 8: First approximation current-field relationship microscopic theory
In the linear approximation does not depend on field, and is cumbersome a function of temperature and frequency.

## Slide 9: How to calculate next order approximation of kernel
Numerical calculation
Take the limit
Low frequency approximation
Dirty limit approximation
Clean limit approximation
Stationary case: Microscopic equation Quasiclassical Eilenberger equations, gauge invariant
Nonstationary case: Microscopic equation Equations are not gauge invariant!

## Slide 10: Static and moving vortices L. Embon, Y. Anahory, Ž.L. Jelić, E. O. Lachman, Y. Myasoedov, M. E. Huber, G. P. Mikitik, A. V. Silhanek, M. V. Milošević, A. Gurevich & E. Zeldov, “Imaging of super-fast dynamics and flow instabilities of superconducting vortices”, Nature Communications volume 8, Article number: 85 (2017)
V. G. Kogan and R. Prozorov, “Interaction between moving Abrikosov vortices in type-II superconductors”, Phys. Rev. B 102, 024506 (2020)
Vortex-vortex potential energy as a function of inter-vortex distance r (static case)
-Modified Bessel function of second kind
V. G. Kogan and N. Nakagawa, “Moving vortices in anisotropic superconductors”, Phys. Rev. B 104, 094523 (2021)
V. G. Kogan and N. Nakagawa,” Current distributions by moving vortices in superconductors”, Phys. Rev. B 104, 094523 (2021)
Two vortices at distance and moving with the same velocity

## Slide 11: Static and moving vortices
V. G. Kogan and N. Nakagawa, “Moving vortices in anisotropic superconductors”, Phys. Rev. B 104, 094523 (2021) . Motion related part of magnetic and electric field is slowly varying
Moving vortex
Vortex at rest

## Slide 12: Oscillating vortex lattice - work in progress:
Oscillation of vortex lattice (or crystal lattice) is governed by its elastic properties [1]
[1] P. Miranovic and V. G. Kogan, “Elastic Moduli of Vortex Lattices within Nonlocal London Model”, Phys. Rev. Lett. 87, 137002 (2001).
Conclusion: Elastic moduli of vortex lattice must depend on oscillation frequency!!
Four independent elastic moduli for vortex lattice: shear, squash, and rotation
Vortex-vortex interaction actually depends on vortex velocities
Assumption that vortex-vortex interaction depends only on distance

## Slide 13: A. Gurevich, T. Kubo, J.A. Sauls, “Challenges and opportunities of superconductor radio fruequency theory for next generation particle accelerators”, Snowmass 21, arXiv:2203.08315
Radio frequency superconductivity is a cornerstone technology for many future HEP particle accelerators and experiments from colliders to proton drivers for neutrino facilities to searches for dark matter
Establishing the Q limit, mechanisms of nonlinear surface resistance and the residual resistance in a nonequilibrium superconductor under a strong RF field.
Establishing the srf breakdown field limit, dynamic superheating field and its dependencies on frequency, temperature and concentration of impurities.
Losses due to trapped vortices and extreme dynamics of ultrafast vortices driven by strong rf Meissner currents in srf cavities.
Optimization of srf performance due to surface nanostructuring of the cavity surface, multilayers and impurity management.